## Slide 2: Workshop How to make a PCB
Eurocircuits.com
The European reference for PCB prototypes & small series
Notes: Good Afternoon, my Name is Steve Jones and this is my colleague Uwe Doerr, we have been invited here by Dr Platt to share with you the black art of Making Printed circuit boards or PCB’s as they are commonly known

## Slide 3: What is PCB pooling and why do we produce like this?
Eurocircuits 2015
Notes: I would now like to look at why Eurocircuits decided to create PCB pooling.

## Slide 4: PCB Pooling
PCB tooling is expensive and required for every production panel
Prototypes and small orders do not fill a complete Production panel of 530mm x 460mm
  The solution: PCB pooling – getting multiple customers wanting the same technology to share the cost of production by optimizing the layout of the production panel with all these designs.
  Result – Eurocircuits offer cost effective prototype solutions meaning happy customers
Notes: PCB tooling films are expensive
Mass production is not set up to handle Protypes and small orders
The solution: PCB pooling – allowing multiple customers to share the cost of production by optimizing the layout, with each customers design forming a part of the whole PCB production panel
  The result – Eurocircuits offer cost effective prototype solutions meaning happy customers

## Slide 5: How to produce a multilayer PCB
Eurocircuits 2015
Notes: Now we have seen the background of Eurocircuits it is important to see how a PCB is made, this helps designers understand and better “design for manufacture”.
Now in a short 30 minute video you can see the process first hand.
I will follow the video with further slides breaking down each stage of the process

## Slide 6: Ingredients for a PCB
Idea
Schematic
CAD design
Gerber & Drill Data (manufacturing data)
PCB fabricator
FR4 (Flame Retardant)
Copper
Prepreg
Finishing – Gold / Solder
Notes: It all starts with the idea,
the idea is made into a schematic,
this is then entered into a CAD package,
this creates the GERBER and Drill data which dectates the physcial form of the idea
Eurocircuits takes these datas and processes them.
Then to create the real board we take FR4 material, with copper on either side, chemically etch the tracks set out by the gerber, and coat the result with an oxident resistant coating for the customer.
FR4 - glass-reinforced epoxy laminate sheets Flame retardant
Pre-preg – Unhardened glass-reinforced epoxy laminate sheets

## Slide 7: How to produce a multilayer PCB
Eurocircuits 2015

## Slide 8: Customer data processing
Order – Have the technology selections been made correctly?
From CAD to CAM - Gerber to PCB production data
PCB production data to photo
tools by laser plotter
Notes: We have seen our film, I would now like to re-iterate the stages in the following slides.
1 –Visualizer checks automatically if key technology points have been selected at the order stage
2) Our front end engineers then verify the data manually to ensure no data errors, that all documents have been checked and meet the order criteria and then create a production file containing all the instructions for all the various production equipment.
3) The data is provided to production and used to create the photoplots, Drill maps, AOI programs

## Slide 9: The inner layers
Exposing the inner layers
  Laminate /Core 700µm thick 35µm/35µm Cu Base material
  Brush or acid Clean Laminate
  Dry film Laminate A photo-sensitive layer
  is applied by a
  Cut Sheet Laminator
Notes: We start with the inner layers
Laminate is an epoxy resin and glass-fibre core with copper foil pre-bonded onto each side
We print the panels in a clean room to make sure that no dust gets onto the surface where it could cause a short or open circuit on the finished PCB.

## Slide 10: The inner layers
Exposing the inner layers
Expose through a
photo tool the
dry film coating
under UV light to define
the copper pattern
Develop the dry film
to remove the
unexposed areas of
the dry film
Notes: The photo sensitive laminate is exposed though a transparent film which has the circuit layout printed on it.
This is then developed and the undeveloped film removed to leave the circuit layout in dry film on the copper layer

## Slide 11: The inner layers
Etching of the inner layers
  Etch away the copper base
  not covered by developed dry
film using an powerful alkali
solution
  Remove the dry resist to
  leave base copper
Notes: The exposed coper is then etched away and only the dry film coper areas are left untouched
The dry film is then removed to leave the circuit in copper.

## Slide 12: The inner layers
Verifying the inner layers
  Make panel registration holes Stamp registration holes in the panel edge by automatic die cutter with optical registration
  Automatic Optical
  Inspection (AOI)
  A Pixel scanner
  utilising the
  production data to
  check for production
  problems, Short,
  Opens, notches etc
Notes: To ensure perfect alignment between all the layers registration holes are stamped into the panel
Before adding more outer layers the inner layers are checked with AOI

## Slide 13: Create and compress the inner layers
Merging of the stack and pressing
Notes: The outer layers of our multilayer consist of sheets of glass cloth pre-impregnated with uncured epoxy resin (prepreg) and a thin copper foil.
The PCB build up is then pressed and heated to bond the outer layers.

## Slide 14: Drilling
Drilling packages pinned and drilling
  First we use an X-ray drill to locate targets in the copper of the inner layers
  Drill holes on high speed CNC machines
Notes: Drilling - First we put a panel of exit material on the drill bed, this stops the drill tearing the copper foil as it comes through the PCB and a sheet of aluminium entry foil on top of the panel to help guide the drill and stop it skidding on the top of the copper foil.
Drilling is a slow process as each hole must be drilled individually. So depending on the drill size we drill a stack of one to three PCB panels together.
We can drill holes down to 100 microns in diameter, to give you an idea of this size, the diameter of a human hair is about 150 microns. Drill change is fully automatic. The machine selects the drill to use from the drill rack, checks that it is the correct size, and then loads it into the drill head.

## Slide 15: Hole plating
Depositing a thin layer of electrically conductive electroless copper or carbon on the hole walls
Notes: Hole plating is a process to ensure all the layers have conductivity - The first step is to deposit a conductive layer over the walls of the hole .
We deposit chemically a layer of copper about 1 micron thick over the walls of the hole (and incidentally across the whole panel)
Panels are carried through a series of chemical and rinsing baths by the overhead crane.
Almost all PCBs with 2 or more copper layers use plated through holes to connect the conductors between the layers.
A good connection needs about 25 microns of copper on the walls of the holes this thickness must be electroplated and controlled precisely

## Slide 16: Exposure of the outer layers
Laminating the outer layers with plating resist (photo sensitive dry film) by means of cut-sheet laminator. Expose and develop
Notes: Again the dry film and photo resist are applied to the outer layer, this time a positive exposure

## Slide 17: Galvanic Process
Galvanic deposition of copper on the conducting paths and holes(+/- 25µm) Cover copper with tin, which then serves as an etch resist.
Notes: We now electroplate the exposed copper with approximately 25-30microns of copper
And then add a layer of tin to protect the copper tracks and pads from the next stage

## Slide 18: Strip - Etch - Strip
Strip - Etch – Strip
  Remove the photoresist
  Etch the exposed copper
  Remove the tin
  resist
Notes: We strip the photoresist leaving exposed copper foil and the traces required, these are then covered by the tin.
We then etch the exposed copper
And Finally removing the tin to leave copper pads and traces exposed

## Slide 19: Soldermask
Applying Soldermask
  Waterfall application
  over the entire panel
  Using a film, expose the
  soldermask with UV light
  and develop to remove
  unexposed areas
Notes: Most boards have an epoxy-ink soldermask
The coating machine simultaneously covers both sides of the panel with the epoxy soldermask ink. The double action ensures that the ink completely encapsulates the copper tracking, typically now 35 – 40 microns higher than the surface of the panel, helping to prevent solder shorting between components during assembly.

## Slide 20: Lead-free surface
Chemical Nickel – Gold (ENIG)
  3-5µm Ni (Nickel)
  0.1-0.2µm Au (Gold)
Chemical Silver
HASL – Hot air Solder Level
Notes: The copper component pads and holes have been left clear of soldermask.
Now we apply a solderable surface finish to protect the copper until the components are soldered onto the board, these can be Nickel Gold, Chemical silver or Lead-free hot-air solder leveling

## Slide 21: Silk screen legend
Print the silk screen by means of digital inkjet
Notes: Component ident is then added to the board

## Slide 22: Electrical Test
Electrically test (netlist) for opens and shorts by flying probe tester.
Notes: At the end of the PCB production process we electrically test every multilayer PCB against the original board data.
This uses 4000 tiny probes like a brush, it builds an electronic map of the PCB from a pre-tested good board. Then it compares each board to be tested with its map. This cuts test times by 90%.

## Slide 23: Profiling – Routing /V-score
Separation of the individual customer PCB’s by milling and/or v-scoring.
Notes: First the machine mills out any small slots or internal cut-outs the cutter follows the path defined in the original tool file.
Next the milling head automatically picks up a 2 mm cutter to mill the outer profile of the PCB

## Slide 24: Quality Assurance
Final inspection and comparison of the intrinsic properties of PCB with the processed data.
Notes: In the last step of the process, quality control, a team of sharp-eyed inspectors give each PCB a final careful check-over, looking for any cosmetic defects like scratches and then measures the panel against the mechanical drawing.

## Slide 25: The Finish Line
Packaging: vacuum-sealing and packing in carton
Send to the customer
A detailed overview can be found on Www.eurocircuits.com under Making a PCB section together with instructional films for PCB manufacturing
Notes: The boards are then Vacuum packed and sent to the customer.
Everything you have seen and heard today you can also find on our website and in addition many helpful Blogs about specific topics

## Slide 26: Eurocircuits workshops
www.Eurocircuits.com free for all to use
  Complete education material available
  Design guidelines
  White papers
  Design templates for Altium and Cadsoft Eagle
  Online design verification
Free onsite workshop presentations for students
For more information on this and everything Eurocircuits can do for you please contact:
Steve.jones@Eurocircuits.com
Tel: +44 7794906982
Notes: The boards are then Vacuum packed and sent to the customer.
Everything you have seen and heard today you can also find on our website and in addition many helpful Blogs about specific topics

## Slide 27
Thanks for your attention
Notes: Thanks for your time today, are there any questions?